Tong Ming Photo Luminescent Tape

FG302 series:  Acrylic type , 5 hours,  Printable, Tearable

Luminescent Value:

The initial lighting source is 1000LX,  Activating time is 15 minutes,

the luminescent value at 5 seconds    ≥   4000  mcd/m2,

the luminescent value at 30 minutes   ≥     15  mcd/m2,

the luminescent value at 60 minutes   ≥      8  mcd/m2,

the luminescent value at 300 minutes  ≥    1.5  mcd/m2,

Service Life: Indoor 8 years, outdoor 5 years

Specification: 1.24m x 45.7m per roll

Available color: light green

Other technical datas:

- Surface Film: Acrylic type

- Thickness of film: 0.125mm, Thickness of Glue:0. 04mm

Thickness of Release Paper: 0.18mm, total thickness of products: 0.345mm

Above thickness is with allowance of 5% more or less

- Weight of Release Paper: 160g/sqm with 5% more or less

- Type of Adhesive: Pressure-Sensitive Type

- Strength of Adhesive: after sticking to the board for 24 hours, at the condition of 0.8kg, 5min, total length: 10cm,  the falling Length≤ 2cm

- Operation temperature: 10 ℃----30 ℃

- Working temperature: -20℃ --- 60℃

(after sticking to the board for at least 7 days)

- Storage temperature: 0 ℃----30 ℃